## Slide 1: Materials for white-LED: efforts for Ab initio Materials Design M. Mikami et al., IOP Conf. Ser.: Mater. Sci. Eng. 1, 012002 (2009) M. Mikami, N. Kijima, B.Bertrand, M.Stankovski, X.Gonze, ibid (in press).
Masayoshi Mikami
Mitsubishi Chemical Group Science & Technology Research Center
Bruno Bertrand*, Martin Stankovski, Xavier Gonze
ETSF/Universite Catholique de Louvain, Belgium
* CERDECAM, Institut Supérieur Industriel ECAM, Belgium
ABINT 2011 Workshop (11-14 April, 2011, Han-sur-Lesse, Belgium)

## Slide 2
Cross-section of present type
(Blue-LED + yellow phosphor)
板東ら,応物, 71(2002),1518
Conventional type:
Blue-LED + yellow phosphor
New (Next) type:
High color rendering types
Blue-LED + yellow & red
Near UV-LED + blue & green & red
Blue-LED + green & red
InGaN chip
YAG phosphor
“www.lightemittingdiodes.org”
B
Y
lacking red
 cool white
New phosphors to be explored !
YAG phosphor
Blue from LED
Yellow from YAG
(typically, Y3Al5O12:Ce3+)
Phosphor-converted white LEDs
Background
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 2
MM

## Slide 3: “Phosphor Handbook” (2006)
β-SiAlON:Eu2+
blue(-green) nitride?!
AlN:Eu2+,Si4+
BaSi7N10:Eu2+
(Sr,Ca)AlSiN3:Eu2+
SrAlSi4N7:Eu2+
Ba3Si6O12N2:Eu2+
Ba3Si6O9N4:Eu2+
Ba1Si2O2N2:Eu2+
LaSi3N5:Ce3+
La3Si6N11:Ce3+
Sr1Si2O2N2:Eu2+
Ca1Si2O2N2:Eu2+
WE NEED GUIDING PRINCIPLES (THEORY) !
+ updates (from literatures)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 3

## Slide 4: from oxides to (oxy)nitrides (or sulfides…)
4f7 ground state
4f65d1
Eabs(Eu2+, A)
EFreeA(Eu2+)
D(2+, A)
εcfs(2+)
εc(2+, A)
isolated Eu2+
in solid “A”
Crystal Field
Splitting
(Likewise with Ce3+)
Notations based on Dorenbos
Eu2+/Ce3+ in “more covalent host”
exhibits longer λem ? ... Not always!
Centroid Shift
“Nephelauxetic”
 Covalency??
Dielectric const., ε
(Refractive index, n)
spectroscopic
polarizability
atomic
polarizability (Dorenbos)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 4
From oxides to (oxy)nitrides (or sulfides)
Background
MM
Notes: The centroid shift c (2+, A), crystal field splitting cfs(2+), redshift D(2+, A), and the lowest energy 4f-5d transition of Eu2+ Eabs(Eu2+, A) are indicated. Similar scheme holds true for Ce3+ ligand field.

## Slide 5: More polarizable (More “MO”), longer λ em
ionic
covalent
Sr2SiO4:Eu
Sr3SiO5:Eu
SrO:Eu
dielectric const.(εxx εyy εzz ) by ABINIT (Density functional Perturbation Theory)
Sr2SiO4: 3.16, 3.28, 3.18
Sr3SiO5: 3.33, 3.33, 3.35
SrO: 3.76, 3.76, 3.76
“3SrO+SiO2”
“SrO”
“2SrO+SiO2”
Yamashita, J.Lumin (1994)
XiXian, Chin. Sci. Bull.(2008)
Park, Appl.Phys.Lett.(2006)
from MM & Kijima, Opt. Mater. (2010)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 5
from oxides to (oxy)nitrides (or sulfides…)
More polarizable (More “MO”), longer λem
Background
Background
MM
Notes: calc: Sr2SiO4 : 3.13, 3.35, 3.21 or 3.16, 3.28, 3.18 v.s. Sr3SiO5: 3.32, 3.32, 3.35 v.s. SrO 3.758
The ionicity of binary oxides and silicates Yale Y. Guo*, C.K. Kuo, Patrick S. Nicholson,
R.R. Reddy et al., Correlation between optical electronegativity, molar refraction, ionicity and density of binary oxides, silicates and minerals

## Slide 6
Notations based on Dorenbos
Coordinate bond length
to be examined !
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 6
4f7 ground state
4f65d1
Eabs(Eu2+, A)
EFreeA(Eu2+)
D(2+, A)
εcfs(2+)
εc(2+, A)
in solid “A”
Crystal Field
Splitting
Centroid Shift
“Nephelauxetic”
 Covalency??
Dielectric const., ε
(Refractive index, n)
spectroscopic
polarizability
from oxides to (oxy)nitrides (or sulfides…)
isolated Eu2+
From oxides to (oxy)nitrides (or sulfides)
Background
MM
Notes: The centroid shift c (2+, A), crystal field splitting cfs(2+), redshift D(2+, A), and the lowest energy 4f-5d transition of Eu2+ Eabs(Eu2+, A) are indicated. Similar scheme holds true for Ce3+ ligand field.

## Slide 7
v.s.
FWHM ∼ 79nm
c.f. AlN:Eu, Si  Eu site (CN = 12)
by Takeda et al.@NIMS, J. Mater. Chem. (2010) 20, 9948
Blue-green !
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 7
from oxides to (oxy)nitrides (or sulfides…)
BaSi7N10:Eu (H.A. Höppe’s Thesis - 2003)
Background
ref. Y.-Q. Li et al. (2009)
Background
MM

## Slide 8
Green luminescence
excited by 400-460nm LED light
Ba3Si6O12N2:Eu2+
small thermal quenching
(Ba,Sr)2SiO4:Eu2+
Emission intensity(20℃=100)
Temperature
Ba
N
Si
New crystal phase
excellent color reproduction
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 8
from oxides to (oxy)nitrides (or sulfides…)
New green phosphor Ba3Si6O12N2:Eu2+
Background
Phosphor
Ba3Si6O12N2:Eu2+
MM

## Slide 9: (Schnick, Hintzen) (Schnick) (Mitsubishi Chemical) (“Sanbornite”)
BaSi2O5 (Ba3Si6O15)
BaSi2O2N2 (Ba3Si6O6N6)
Ba3Si6O9N4
Ba3Si6O12N2
12 anions/(Ba3+Si6)
13 anions
14 anions
15 anions
Question:
N-rich
⇒ more polarizable
⇒ longer λ em ?
n=1.90-1.95
n=1.81
n=1.76
n=1.65
N-rich
larger refractive index n ?
( calculation)
The missing piece
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 9
MM
Phosphor
Ba3Si6O12N2:Eu2+

## Slide 10
Ba3Si6O12N2:Eu
Ba3Si6O9N4:Eu
PL peak ∼ 530nm (Green)
strong luminescence@R.T.
PL peak ∼ 480nm (Blue-green)
quenching @ R.T.
Uheda et al. (2007), MM et al. (2009); see also, C. Braun et al.(2010)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 10
from oxides to (oxy)nitrides (or sulfides…)
Ba3Si6O12N2 / Ba3Si6O9N4 Eu f-d emission
MM
Phosphor
Ba3Si6O12N2:Eu2+

## Slide 11
B.Dierre et al. (2007)
configurational coordinate
auto-ionization
heat
absorption
emission
e - release
heat
from oxides to (oxy)nitrides (or sulfides…)
Thermal quenching mechanism
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 11
Difficult to explain thermal quenching with configurational coordinate diagram…
Natural to explain with auto-ionization mechanism
MM
Phosphor
Ba3Si6O12N2:Eu2+
Notes: Xie alpha-SiAlON paper to be cited here ?

## Slide 12
from oxides to (oxy)nitrides (or sulfides…)
PL/PLE of Ba3Si6O12N2 & Ba3Si6O9N4
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 12
Stokes shift (cm-1)
Ba3Si6O12N2:Eu 2790
Ba3Si6O9N4:Eu 3230
Difficult to explain
thermal quenching with
configurational coordinate diagram…
Natural to explain with
auto-ionization mechanism
MM
Phosphor
Ba3Si6O12N2:Eu2+
Notes: “Entities should not be multiplied beyond necessity.“ "plurality should not be posited without necessity".
2788 & 3232
Occam's razor: "Given two equally predictive theories, choose the simplest."

## Slide 13
Isolated Eu2+
Eu2+ in the bulk
Bulk valence band
Bulk conduction band
How to determine the luminescence mechanism from DFT ?
1) Model for photo-emission
Energy gap between the lowest 5d and 4f states of Europium impurities within the host gap
4f
5d
from oxides to (oxy)nitrides (or sulfides…)
An empirical model
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 13
BB
Phosphor
Ba3Si6O12N2:Eu2+

## Slide 14
Isolated Eu2+
Eu2+ in the bulk
Bulk valence band
Bulk conduction band
How to determine the luminescence mechanism from DFT ?
1) Model for photo-emission
Energy gap between the lowest 5d and 4f states of Europium impurities within the host gap
2) Model for thermal quenching
Auto-ionization of Eu2+ → Eu3+ + e-
Energy gap between 5d levels of Eu and the conduction band.
4f
5d
P. Dorenbos J.Phys.Cond.Mat.17 (2005)
from oxides to (oxy)nitrides (or sulfides…)
An empirical model
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 13
BB
Phosphor
Ba3Si6O12N2:Eu2+

## Slide 15
PAW atomic data for Europium
Position of the 4f and 5d orbitals of Europium
Position and concentration of Eu impurities
Electronic structure of host material
Bulk valence band
Bulk conduction band
Crystalline structure of host material
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using Abinit : general overview
Background
Calculation for the host Ba3Si6O12N2
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 14
BB
Phosphor
Ba3Si6O12N2:Eu2+

## Slide 16
Bulk valence band
Bulk conduction band
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using abinit : DFT calculation
Background
Host material
Crystal structure
Crystalline structure of host material
↓
Ground state structural relaxation
Calculation for the host Ba3Si6O12N2
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 15
BB

## Slide 17
Ba
N
Si
O
Lattice parameters :
DFT (GGA) with PAW atomic data
Crystalline structure of Ba3Si6O12N2 by Abinit
 | Parameter a (Å) | Parameter c (Å)
Experimental | 7.5046(8) | 6.4703(5)
[1] Ba without semi-core states | 7.597 | 6.575
[2] Ba with semi-core states | 7.610 | 6.552
Ba
Crystalline structure of Ba3Si6O12N2 by Abinit
New crystal structure for oxynitride
Host material
Crystal structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 16
BB
[1] M. Mikami et al., Key Engineering Material Vol. 403 (2009).
[2] M. Mikami, N. Kijima, B. Bertrand, M. Stankovski and X. Gonze, In press

## Slide 18
Ba
N
Si
O
Lattice parameters :
DFT (GGA) with PAW atomic data
Crystalline structure of Ba3Si6O12N2 by Abinit
PAW atomic data for Barium
Results are coherent with experimental data whether semi-core states are used or not
[1] M. Mikami et al., Key Engineering Material Vol. 403 (2009).
[2] M. Mikami, N. Kijima, B. Bertrand, M. Stankovski and X. Gonze, In press
 | Parameter a (Å) | Parameter c (Å)
Experimental | 7.5046(8) | 6.4703(5)
[1] Ba without semi-core states | 7.597 | 6.575
[2] Ba with semi-core states | 7.610 | 6.552
Ba
Crystalline structure of Ba3Si6O12N2 by Abinit
New crystal structure for oxynitride
Host material
Crystal structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 16
BB

## Slide 19
Bulk valence band
Bulk conduction band
Crystalline structure of host material
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using abinit : GW + PAW calculation
Background
Calculation for the host Ba3Si6O12N2
Electronic structure of host material
↓
G0W0 + PAW calculation
Host material
Electronic structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 17
BB

## Slide 20
Highly covalent oxynitride phosphors
Large effects of the screening on the optical properties
Density functional theory (DFT) fails seriously in the description of band gaps or photoemission.
The standard way to go beyond is to invoke many-body perturbation theory (MBPT).
 | DFT indirect gap (eV) | G0W0 indirect gap (eV) | Experimental gap (eV)
Ba3Si6O12N2 | 4.589 | 6.772 | 7.05 ± 0.25
Why is it mandatory to invoke a GW correction ?
from oxides to (oxy)nitrides (or sulfides…)
Using a GW calculation
Background
Host material
Electronic structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 18
BB

## Slide 21
Γ
A
M
L
K
H
M
Band energy (eV)
DFT Gap :
4.589 eV
Zoom on the state around the band gap
from oxides to (oxy)nitrides (or sulfides…)
Host material
Electronic structure
GW correction to DFT
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 19
BB

## Slide 22
Γ
A
M
L
K
H
M
GW correction to DFT
Host material
Electronic structure
Band energy (eV)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 19
BB

## Slide 23
Γ
A
M
L
K
H
M
G0W0 Gap :
6.772 eV
Band energy (eV)
GW correction to DFT
Host material
Electronic structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 19
BB

## Slide 24
Ba3Si6O12N2:Eu
Ba3Si6O9N4:Eu
PL peak ∼ 530nm (Green)
strong luminescence@R.T.
PL peak ∼ 480nm (Blue-green)
quenching @ R.T.
Uheda et al. (2007), MM et al. (2009); see also, C. Braun et al.(2010)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 20
from oxides to (oxy)nitrides (or sulfides…)
Ba3Si6O12N2 / Ba3Si6O9N4 Eu f-d emission
Background
Host material
Electronic structure
BB

## Slide 25
 | GW indirect gap (eV) | GW direct gap at Γ (eV) | Experimental gap (eV)
1) Ba3Si6O12N2 | 6.772 | 7.092 | 7.05 ± 0.25
2) Ba3Si6O9N4 | 6.443 | 6.698 | 
Ba3Si6O12N2 : Grid of 30 k-points with a (controlled) numerical error of 0.06 eV.
Ba3Si6O9N4 : Grid of 14 k-points with a (controlled) numerical error of 0.06 eV.
from oxides to (oxy)nitrides (or sulfides…)
Comparison of energy gaps
Host material
Electronic structure
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 21
Comparison of materials with similar composition but different thermal quenching
1) Ba3Si6O12N2 + Eu2+ : Strong luminescence at room temperature
2) Ba3Si6O9N4 + Eu2+ : Little luminescence at room temperature
Our results are in agreement with the auto-ionization model to explain the better thermal properties of Ba3Si6O12N2
BB
Nband (SCR) : 423
Nband (SIG) : 450
Gwencomp (SCR) : 2.5
Gwencomp (SIG) : 2.0
Ecuteps : 7 Ha
Ecutsigx : 20 Ha

## Slide 26
Bulk valence band
Bulk conduction band
Bulk valence band
Bulk conduction band
6.772 eV
6.443 eV
Ba3Si6O12N2
Ba3Si6O9N4
4f
5d
4f
5d
Host material
Electronic structure
Comparison of energy gap
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 22
BB

## Slide 27
Electronic structure of host material
Bulk valence band
Bulk conduction band
Crystalline structure of host material
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using abinit : PAW atomic data
Background
Calculation for the host Ba3Si6O12N2
PAW atomic data for Europium
↓
Semi-core states
PAW
Atomic data
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 23
BB

## Slide 28
Europium
Ba3Si6O12N2 | G0W0 indirect gap (eV) | G0W0 direct gap (eV)
4d semi-core | 6.772 Γ - A | 7.092 Γ
Without semi-core state | 3.740 L - A | 3.807 L
Experimental | 7.05 | 
Semi-core : 4d10 5s2
Valence : 5p6 6p2
Barium
Semi-core : 4d10 5s2
Valence : 5p6 4f7 6p2
Test of the G0W0 correction to EuO : - Introduction of semi-core 4d10 states - Problems with the correction of 4f states
from oxides to (oxy)nitrides (or sulfides…)
Construction of PAW atomic data
Background
PAW
Atomic data
Background
PAW
Atomic data
Semi-core states are required in order to make sensible the G0W0 correction.
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 24
BB
Notes: Similar conclusions also apply to simple compounds like BaO

## Slide 29
PAW atomic data for Europium
Electronic structure of host material
Bulk valence band
Bulk conduction band
Crystalline structure of host material
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using abinit
Background
Calculation for the host Ba3Si6O12N2
Position and concentration of Eu impurities
↓
Spin polarized GGA(+U)
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 25
Phosphors
Eu impurities
BB

## Slide 30
Ba
or doping Eu
N
Si
O
Onxynitride layer :
SiO3N tetrahedra
Ba-(O,N) or Eu-(O,N)
Ba-(O) or Eu-(O)
Eu impurities act as luminescence centers
from oxides to (oxy)nitrides (or sulfides…)
Adding Europium impurities
Background
Background
Background
Phosphors
Eu impurities
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 26
BB

## Slide 31
from oxides to (oxy)nitrides (or sulfides…)
Non equivalent positions
BB
Background
Background
Background
Phosphors
Eu impurities
Europium substitutes to Barium atoms in two possible non equivalent positions
O
O
O
O
O
O
O
O
O
O
O
O
N
N
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 27
Eu
Eu

## Slide 32
PAW atomic data for Europium
Position and concentration of Eu impurities
Electronic structure of host material
Bulk valence band
Bulk conduction band
Crystalline structure of host material
Calculation for Ba3Si6O12N2 : Eu2+
from oxides to (oxy)nitrides (or sulfides…)
Using abinit : Perspectives
Background
Perspectives
Calculation for the host Ba3Si6O12N2
Perspective :
Position of the 4f and 5d states of Europium
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 28
BB

## Slide 33
Ba3Si6O12N2:Eu
Ba3Si6O9N4:Eu
conduction bands
Eu 4f
Eu 5d
Eu-O6
cluster
Eu-O6
cluster
Eu2+Eu3++ e- (auto-ionization)
Eu-N
ligand
Eu-N
ligand
Green PL
peak ∼ 530nm
Blue-Green PL
peak ∼ 480nm
valence bands
Eu 4f
Eu 5d
6.772 eV (GW)
6.443eV (GW)
proposed by MM et al.(2009): based on Dorenbos scheme (J.Phys.Cond.Mat.17, 2005)
from oxides to (oxy)nitrides (or sulfides…)
The difference of EU PL : a model
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 29
MM
Perspectives
Notes: Dorenbos, J. Phys. Condens. Matter 17, 8103 (2005)

## Slide 34
Eu 4f
Eu 5d
Eu-N
ligand
valence bands
from oxides to (oxy)nitrides (or sulfides…)
Towards a validation of the model
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 30
BB
Ba3Si6O12N2:Eu
conduction bands
Eu-O6
cluster
Zoom on the bottom of the conduction band - Preliminary results
Partial density of states
Eu d channel
Eu s channel
Ba d channel
Ba s channel
Eu
O
N
Perspectives
Energy (Ha)
Notes: Dorenbos, J. Phys. Condens. Matter 17, 8103 (2005)

## Slide 35
M.Mikami & B.Bertrand – ABINIT 2011 Workshop, Han-sur-Lesse - 31
Conclusion
New crystal structure for oxynitride
Scientific interest
Luminescence properties of rare-earth doping oxynitrides phosphors
    Emission and absorption spectra
    Thermal quenching
Numerical Challenge
Electronic structure of Ba3Si6O12N2 phosphor
  Current : G0W0 with PAW atomic data including semi-core and 4f states
  Future : Electron-phonon interaction
Industry ► Reducing the cost of R&D
  Discovery of new compounds
  Prediction of properties before synthesis
BB

## Slide 36
Acknowledgments
(MCRC) for development/analysis of our phosphors, encouragement from theoretical Gr.
Kyota Uheda, Satoshi Shimooka, Yasuo Shimomura, Tomoyuki Kurushima,
Takatoshi Seto, Hiromu Watanabe, Toshio Akai, Masaki Takashima,
Yutaka Sasaki, Motoyuki Shigeiwa, Kaoru Okamoto, Hiroyuki Imura,
Katsuya Kanda, Shinichiro Nakamura
(ETSF/Universite Catholique de Louvain) for PAW-GW calc. & build system of ABINIT
Matteo Giantomassi, Alain Jacques, Gian-Marco Rignanese, Yann Pouillon
BB, MS, XG: financial support from the European Union, 7th Framework Programme (Grant Agreement 211956 ETSF I3 e-Infrastructure project), the Agentschap voor Innovatie door Wetenschap en Technologie (IWT project N°080023 ISIMADE), as well as the Walloon region Belgium (RW project N°816849, WALL-ETSF)

## Slide 37: A photo from Sendai (Tohoku University)
“Prof. Kotaro Honda in Director office is keeping up
even after breakdown of the table by Tohoku-Pacific
Ocean Earthquake on March 11 2011”
Notes: http://www.imr.tohoku.ac.jp/jpn/about/fukkyu/fukkyu_index.html